### Operating Instructions 1-10DE99

Equipment Calibration

Section 6

6.1	Equipment Calibration

### Operating Instructions 1-10DE99

Equipment Calibration

6.1 Equipment Calibration

The following list of recommended set-up adjustments and reference values should be used to help obtain the optimal performance from your blast cleaning system.  These should be used as starting points and can be fine-tuned after trial and observation.

CAUTION: CALIBRATION OF ITEMS 1, 2, 6 AND 7 MUST BE MADE WITH ALL ELECTRICAL DISCONNECTS IN THE “OFF” POSITION.  ALL MOVING PARTS MUST BE COMPLETELY STOPPED BEFORE MAKING ANY ADJUSTMENTS OR PERFORMING MAINTENANCE.

- Blast Housing Height - The bottom of the blast housing (magnets) should be between 1/8” to 1/2” above the surface being cleaned.  A smaller clearance can be obtained for smooth surfaces and the height may need to be higher for rough surfaces.

- Control Cage Setting - See Section 5, “Setting the Correct Blast Pattern”; figures A, B and C.

- Abrasive Selection Recommendations (Steel Shot Size)

- Brush blast of smooth concrete:  S-170 to S-280 (smaller size will produce a brighter etch)

- Rough concrete etch for coatings:  S-330 to S-460

- Heavy concrete removal:  S-460

- Cleaning scale or paint on steel:  S-460

- Travel Speed Suggestions (Speed Control Potentiometer)

- Brush blasting:  40 to 80 (higher speeds)

- Heavy concrete blast:  15 to 40 (medium speeds)

- Steel surface cleaning:  10 to 15 (slow speeds)

- Exhaust Hose Length - Fifty feet of 3-inch diameter exhaust hose; longer or shorter sections of hose may affect abrasive consumption or abrasive cleaning.  Contact your Blastrac representative before changing the exhaust hose length.

### Operating Instructions 1-10DE99

Equipment Calibration

6.1 Cont’d

- Dust Collector Pulse Timer - Set for approximately 10 seconds for concrete cleaning; 15 seconds for steel cleaning.

- Compressor Pressure Setting - 80 PSI max. The unloader adjustment determines pressure (30 PSI drop for Pulse).

- Pressure Drop Across Filters - Minihelic gauge should read between 1 and 4 inches.  An indication above 4 indicates that the filters are dirty.

- Dust Bin Change Interval. - Inspect at 1/2-hour intervals to estimate fill time.  Do not allow dust bin to overfill.